SECTION 074213.13 - FORMED METAL WALL PANELS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on Masterworks/Single-File Formatting/Toggle/Editor's Notes.

Revise this Section by deleting and inserting text to meet Project-specific requirements.

This Section uses the term "Architect." Change this term to match that used to identify the design professional as defined in the General and Supplementary Conditions.

- GENERAL

      - RELATED DOCUMENTS

Retain or delete this article in all Sections of Project Manual.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 01 Specification Sections, apply to this Section.

      - SUMMARY

        - Section Includes:

          - Metal liner panels.

        - Related Sections:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 074213.16 "Metal Plate Wall Panels" for solid metal plate wall panels.

          - Section 074213.19 "Insulated Metal Wall Panels" for foamed-in-place, laminated and honeycomb insulated metal wall panels.

          - Section 074213.23 "Metal Composite Material Wall Panels" for metal-faced composite wall panels.

          - Section 074293 "Soffit Panels" for metal panels used in horizontal soffit applications.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 13100 "Project Management and Coordination."

Retain subparagraphs below if additional requirements are necessary; revise to include more specific information about conference.

          - Meet with Owner, Architect, Owner's insurer if applicable, metal panel Installer, metal panel manufacturer's representative, structural-support Installer, and installers whose work interfaces with or affects metal panels, including installers of doors, windows, and louvers.

          - Review and finalize construction schedule and verify availability of materials, Installer's personnel, equipment, and facilities needed to make progress and avoid delays.

          - Review methods and procedures related to metal panel installation, including manufacturer's written instructions.

          - Examine support conditions for compliance with requirements, including alignment between and attachment to structural members.

          - Review flashings, special siding details, wall penetrations, openings, and condition of other construction that affect metal panels.

          - Review governing regulations and requirements for insurance, certificates, and tests and inspections if applicable.

          - Review temporary protection requirements for metal panel assembly during and after installation.

          - Review of procedures for repair of metal panels damaged after installation.

          - Document proceedings, including corrective measures and actions required, and furnish copy of record to each participant.

      - ACTION SUBMITTALS

        - Product Data: For each type of product.

          - Include construction details, material descriptions, dimensions of individual components and profiles, and finishes for each type of panel and accessory.

        - Sustainable Design Submittals:

          - Product Data: For recycled content, indicating postconsumer and preconsumer recycled content and cost.

        - Shop Drawings:

          - Include fabrication and installation layouts of metal panels; details of edge conditions, joints, panel profiles, corners, anchorages, attachment system, trim, flashings, closures, and accessories; and special details.

          - Accessories: Include details of the flashing, trim, and anchorage systems, at a scale of not less than 3" = 1'-0" (1:5).

        - Calculations:

          - Include calculations with registered engineer seal, verifying wall panel and attachment method resist wind pressures imposed on it pursuant to applicable building codes.

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs below for two-stage Samples.

        - Samples for Initial Selection: For each type of metal panel indicated with factory-applied finishes.

          - Include Samples of trim and accessories involving color selection.

        - Samples for Verification: For each type of exposed finish, prepared on Samples of size indicated below:

          - Metal Panels: 12 inches (305 mm) long by actual panel width. Include fasteners, closures, and other metal panel accessories.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

        - Qualification Data: For Installer and Manufacturer.

        - Product Test Reports: For each product, for tests performed by a qualified testing agency.

Retain "Field quality-control reports" Paragraph below if Contractor is responsible for field quality-control testing and inspecting.

        - Field quality-control reports.

        - Sample Warranties: For special warranties.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data: For metal panels to include in maintenance manuals.

      - QUALITY ASSURANCE

        - Installer Qualifications: An entity that employs installers and supervisors who are trained and approved by manufacturer.

        - Manufacturer Qualifications: Company specializing in Architectural Sheet Metal Products.

        - Mockups: Build mockups to verify selections made under Sample submittals and to demonstrate aesthetic effects and set quality standards for fabrication and installation.

Retain first subparagraph below for large-scale mockup. Indicate portion of building represented by mockup on Drawings or draw mockup as separate element. Revise to suit Project or if larger mockup is needed for field performance testing.

          - Build mockup of typical metal panel assembly [as shown on Drawings] <Insert size>, including [corner,] [soffits,] supports, attachments, and accessories.

          - Water-Spray Test: Conduct water-spray test of metal panel assembly mockup, testing for water penetration according to AAMA 501.2.

Retain first subparagraph below if mockups are not only for establishing appearance factors.

          - Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Architect specifically approves such deviations in writing.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver components, metal panels, and other manufactured items so as not to be damaged or deformed. Package metal panels for protection during transportation and handling.

        - Unload, store, and erect metal panels in a manner to prevent bending, warping, twisting, and surface damage.

        - Stack metal panels horizontally on platforms or pallets, covered with suitable weathertight and ventilated covering. Store metal panels to ensure dryness, with positive slope for drainage of water. Do not store metal panels in contact with other materials that might cause staining, denting, or other surface damage.

        - Remove strippable protective covering on metal panels as panels are being installed. Do not leave the film on installed panels.

      - FIELD CONDITIONS

        - Weather Limitations: Proceed with installation only when existing and forecasted weather conditions permit assembly of metal panels to be performed according to manufacturers' written instructions and warranty requirements.

      - COORDINATION

        - Coordinate metal panel installation with rain drainage work, flashing, trim, construction of soffits, and other adjoining work to provide a leakproof, secure, and noncorrosive installation.

      - WARRANTY

When warranties are required, verify with Owner's counsel that special warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

        - Galvalume Substrate  Warranty: Manufacturer's standard form in which manufacturer agrees to repair or replace components of metal panel systems that fail in materials or workmanship within specified warranty period.

          - Failures include, but are not limited to, the following:

            - Structural failures including rupturing or perforating.

            - Deterioration of metals and other materials beyond normal weathering.

          - Warranty Period: 20 years and 6 months from date of Substantial Completion.

        - Special Warranty on Panel Finishes: Manufacturer's standard form in which manufacturer agrees to repair finish or replace metal panels that show evidence of deterioration of factory-applied finishes within specified warranty period.

Usually retain "Exposed Panel Finish" Subparagraph below for fluoropolymer finishes; verify availability with manufacturer.

          - Exposed Panel Finish: Deterioration includes, but is not limited to, the following:

            - Color fading more than 5 Hunter units when tested according to ASTM D 2244.

            - Chalking in excess of a No. 8 rating when tested according to ASTM D 4214.

            - Cracking, chipping, peeling, or failure of paint to adhere to bare metal.

          - Finish Warranty Period: 20 years from date of Substantial Completion.

- PRODUCTS

      - PERFORMANCE REQUIREMENTS

Retain "Recycled Content" Paragraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

        - Recycled Content: Postconsumer recycled content plus one-half of preconsumer recycled content not less than 29 percent.

In completing this section, refer to the chart at http://www.berridge.com/technical/testing-summary-chart/ for technical guidance based on the panel profile being utilized.

        - Structural Performance: Provide metal panel systems capable of withstanding the effects of the following loads, based on testing according to ASTM E 330:

          - Wind Loads: As indicated on Drawings.

          - Deflection Limits: For wind loads, no greater than [1/180] [1/240] <Insert deflection> of the span.

      - METAL LINER PANELS

        - General: Provide factory-formed metal liner panels designed for interior side walls and field assembled by lapping and interconnecting side edges of adjacent panels and mechanically attaching through panel to supports using concealed fasteners in side laps. Include accessories required for a complete installation.

Insert drawing designation for each product required. Use these designations on Drawings to identify each product.

        - Metal Liner Panels <Insert drawing designation>: Solid panels formed with a flat pan between panel edges; with a flush joint between panels.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Berridge Manufacturing Company; Thin Line or comparable product by one of the following:

            - <Insert manufacturer’s name>.

          - Metallic-Coated Steel Sheet: Aluminum-zinc alloy-coated steel sheet complying with ASTM A 792/A 792M, Class AZ50 (Class AZM150) coating designation; structural quality. Prepainted by the coil-coating process to comply with ASTM A 755/A 755M.

            - Nominal Thickness: 0.024 inch (0.61 mm).

            - Surface: [Smooth, flat] [Stucco Embossed] [Woodgrain Embossed] finish.

            - Exterior Finish: [Two-coat fluoropolymer] [Mica fluoropolymer] [Metallic fluoropolymer]

Refer to color Chart located at http://www.berridge.com/colors/ for options.

            - Color: [As indicated by manufacturer's designations] [Match Architect's samples] [As selected by Architect from manufacturer's full range] <Insert color>.

          - Panel Coverage: 3.625 inches (92 mm).

          - Seam Height: 0.375 inches (10 mm).

      - UNDERLAYMENT MATERIALS

Retain appropriate paragraphs in this article for metal wall panels applied over sheathing. Self-adhering, high-temperature underlayment may be applied only at wall opening flashing conditions vulnerable to leakage, with felt applied over the remainder of the wall; or underlayment may be applied over the entire wall area.

Underlayments listed in "Self-Adhering, High-Temperature Underlayment" Paragraph below are suitable for higher temperatures associated with metal wall application. Revise if high-temperature underlayments are not required. Verify, with underlayment manufacturer, acceptability for use on wall applications and directly over corrugated metal deck.

For a list of approved underlayment manufacturers supported by Berridge, please refer to the following: http://www.berridge.com/wp-content/uploads/2014/06/Approved-Materials-Form-11-4-13.pdf.

        - Self-Adhering, High-Temperature Underlayment: Provide self-adhering, cold-applied, sheet underlayment, a minimum of 40 mils (1.02 mm) thick, consisting of slip-resistant, polyethylene-film top surface laminated to a layer of butyl or SBS-modified asphalt adhesive, with release-paper backing. Provide primer when recommended by underlayment manufacturer.

          - Manufacturers: Subject to compliance with requirements, provide products by one of the following:

            - Grace Ultra

            - Mid-States Asphalt Quick Stick HT Pro

            - Polyglass Polystick MTS

            - Soprema Lastobond Shield HT

            - Tamko TW Underlayment or TW Metal & Tile Underlayment

            - <Insert manufacturer’s name>.

          - Thermal Stability: Stable after testing at 240 deg F (116 deg C); ASTM D 1970.

          - Low-Temperature Flexibility: Passes after testing at minus 20 deg F (29 deg C); ASTM D 1970.

Retain "Felt Underlayment" Paragraph below if not using self-adhering, high-temperature underlayment over the entire roof area.

        - Felt Underlayment: ASTM D 226/D 22M, Type II (No. 30), asphalt-saturated organic felts.

      - MISCELLANEOUS MATERIALS

If 16 gage subframing is required, then choose ASTM A653.  If 22 gage or 24 gage subframing is required, then choose ASTM A792.

        - Miscellaneous Metal Subframing and Furring: ASTM C 645, cold-formed, metallic-coated steel sheet, ASTM A 653/A 653M, G90 (Z275) hot-dip galvanized coating designation or ASTM A 792/A 792M, Class AZ50 (Class AZM150) aluminum-zinc-alloy coating designation unless otherwise indicated. Provide manufacturer's standard sections as required for support and alignment of metal panel system.

Retain panel accessories, flashing, and trim as required and coordinate with those specified in Section 076200 "Sheet Metal Flashing and Trim."

        - Panel Accessories: Provide components required for a complete, weathertight panel system including trim, copings, fasciae, mullions, sills, corner units, clips, flashings, sealants, gaskets, fillers, closure strips, and similar items. Match material and finish of metal panels unless otherwise indicated.

          - Closures: Provide closures at eaves and rakes, fabricated of same metal as metal panels.

          - Backing Plates: Provide metal backing plates at panel end splices, fabricated from material recommended by manufacturer.

          - Closure Strips: Closed-cell, expanded, cellular, rubber or crosslinked, polyolefin-foam or closed-cell laminated polyethylene; minimum 1-inch- (25-mm-) thick, flexible closure strips; cut or premolded to match metal panel profile. Provide closure strips where indicated or necessary to ensure weathertight construction.

        - Flashing and Trim: Provide flashing and trim formed from same material as metal panels as required to seal against weather and to provide finished appearance. Locations include, but are not limited to, bases, drips, sills, jambs, corners, endwalls, framed openings, rakes, fasciae, parapet caps, soffits, reveals, and fillers. Finish flashing and trim with same finish system as adjacent metal panels.

        - Panel Fasteners: Self-tapping screws designed to withstand design loads. Provide exposed fasteners with heads matching color of metal panels by means of factory-applied coating. Provide EPDM or PVC sealing washers for exposed fasteners.

For approved sealant guidance refer to the approved list at http://www.berridge.com/wp-content/uploads/2014/06/Approved-Materials-Form-11-4-13.pdf.

        - Panel Sealants: Provide sealant type recommended by manufacturer that are compatible with panel materials, are nonstaining, and do not damage panel finish.

          - Sealant Tape: Pressure-sensitive, 100 percent solids, gray polyisobutylene compound sealant tape with release-paper backing. Provide permanently elastic, nonsag, nontoxic, nonstaining tape 1/2 inch (13 mm) wide and 1/8 inch (3 mm) thick.

          - Joint Sealant: ASTM C 920; elastomeric polyurethane or silicone sealant; of type, grade, class, and use classifications required to seal joints in metal panels and remain weathertight; and as recommended in writing by metal panel manufacturer.

          - Butyl-Rubber-Based, Solvent-Release Sealant: ASTM C 1311.

      - FABRICATION

        - General: Fabricate and finish metal panels and accessories at the factory, by manufacturer's standard procedures and processes, as necessary to fulfill indicated performance requirements demonstrated by laboratory testing. Comply with indicated profiles and with dimensional and structural requirements.

        - Provide panel profile, including major ribs and intermediate stiffening ribs, if any, for full length of panel.

        - Sheet Metal Flashing and Trim: Fabricate flashing and trim to comply with manufacturer's recommendations and recommendations in SMACNA's "Architectural Sheet Metal Manual" that apply to design, dimensions, metal, and other characteristics of item indicated.

          - Form exposed sheet metal accessories that are without excessive oil canning, buckling, and tool marks and that are true to line and levels indicated, with exposed edges folded back to form hems.

          - Seams for Aluminum: Fabricate nonmoving seams with flat-lock seams. Form seams and seal with epoxy seam sealer. Rivet joints for additional strength.

          - Seams for Other Than Aluminum: Fabricate nonmoving seams in accessories with flat-lock seams. Tin edges to be seamed, form seams, and solder.

          - Sealed Joints: Form nonexpansion, but movable, joints in metal to accommodate sealant and to comply with SMACNA standards.

          - Conceal fasteners and expansion provisions where possible. Exposed fasteners are not allowed on faces of accessories exposed to view.

          - Fabricate cleats and attachment devices from same material as accessory being anchored or from compatible, noncorrosive metal recommended in writing by metal panel manufacturer.

            - Size: As recommended by SMACNA's "Architectural Sheet Metal Manual" or metal wall panel manufacturer for application but not less than thickness of metal being secured.

      - FINISHES

        - Protect mechanical and painted finishes on exposed surfaces from damage by applying a strippable, temporary protective covering before shipping.

        - Appearance of Finished Work: Variations in appearance of abutting or adjacent pieces are acceptable if they are within one-half of the range of approved Samples. Noticeable variations in same piece are not acceptable. Variations in appearance of other components are acceptable if they are within the range of approved Samples and are assembled or installed to minimize contrast.

        - Steel Panels and Accessories:

Retain one exposed fluoropolymer finish from subparagraphs below. Verify availability of finishes for products specified. If retaining more than one, indicate location of each on Drawings or by inserts. To obtain a proprietary finish system, insert names of coating manufacturers and products.

          - Two-Coat Fluoropolymer: AAMA 621. Fluoropolymer finish containing not less than 70 percent PVDF resin by weight in color coat applied by panel manufacturer on a continuous coil coating line, with a top side dry film thickness of 0.75± 0.05 mil (0.019± 0.0013 mm) over 0.2± 0.05 mil (0.05± 0.0013 mm) primer coat, to provide a total dry film thickness of 0.95± 0.10 mil (0.024± 0.0025 mm). Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

          - Mica Fluoropolymer: AAMA 621. Two-coat fluoropolymer finish with suspended mica flakes containing not less than 70 percent PVDF resin by weight in color coat applied by panel manufacturer on a continuous coil coating line, with a top side dry film thickness of 0.75± 0.05 mil (0.019± 0.0013 mm) over 0.2± 0.05 mil (0.05± 0.0013 mm) primer coat, to provide a total dry film thickness of 0.95± 0.10 mil (0.024± 0.0025 mm). Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

          - Metallic Fluoropolymer: AAMA 621. Two-coat fluoropolymer finish with suspended metallic flakes containing not less than 70 percent PVDF resin by weight in color coat applied by panel manufacturer on a continuous coil coating line, with a top side dry film thickness of 0.75± 0.05 mil (0.019± 0.0013 mm) over 0.2± 0.05 mil (0.05± 0.0013 mm) primer coat, to provide a total dry film thickness of 0.95± 0.10 mil (0.024± 0.0025 mm). Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

Finish in "Concealed Finish" Subparagraph below is frequently used as a factory finish for interior surfaces.

          - Concealed Finish: Apply pretreatment and manufacturer's standard white or light-colored acrylic or polyester backer finish consisting of prime coat and wash coat with a minimum total dry film thickness of 0.35 mil (0.009 mm).

        - Aluminum Panels and Accessories:

Retain one fluoropolymer finish from subparagraphs below. Verify availability of finishes for products specified. If retaining more than one, indicate location of each on Drawings or by inserts. To obtain a proprietary finish system, insert names of coating manufacturers and products.

Revise or insert additional testing requirements in three fluoropolymer subparagraphs below if performance levels indicated in AAMA 2605 are insufficient.

          - Two-Coat Fluoropolymer: AAMA 2605. Fluoropolymer finish containing not less than 70 percent PVDF resin by weight in color coat applied by panel manufacturer on a continuous coil coating line, with a top side dry film thickness of 0.75± 0.05 mil (0.019± 0.0013 mm) over 0.2± 0.05 mil (0.05± 0.0013 mm) primer coat, to provide a total dry film thickness of 0.95± 0.10 mil (0.024± 0.0025 mm).  Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

          - Mica Fluoropolymer: AAMA 2605. Two-coat fluoropolymer finish with suspended mica flakes containing not less than 70 percent PVDF resin by weight in color coat applied by panel manufacturer on a continuous coil coating line, with a top side dry film thickness of 0.75± 0.05 mil (0.019± 0.0013 mm) over 0.2± 0.05 mil (0.05± 0.0013 mm) primer coat, to provide a total dry film thickness of 0.95± 0.10 mil (0.024± 0.0025 mm). Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

          - Metallic Fluoropolymer: AAMA 2605. Two-coat fluoropolymer finish with suspended metallic flakes containing not less than 70 percent PVDF resin by weight in color coat applied by panel manufacturer on a continuous coil coating line, with a top side dry film thickness of 0.75± 0.05 mil (0.019± 0.0013 mm) over 0.2± 0.05 mil (0.05± 0.0013 mm) primer coat, to provide a total dry film thickness of 0.95± 0.10 mil (0.024± 0.0025 mm). Prepare, pretreat, and apply coating to exposed metal surfaces to comply with coating and resin manufacturers' written instructions.

- EXECUTION

      - EXAMINATION

        - Examine substrates, areas, and conditions, with Installer present, for compliance with requirements for installation tolerances, metal panel supports, and other conditions affecting performance of the Work.

Retain one or both subparagraphs below.

          - Examine wall framing to verify that girts, angles, channels, studs, and other structural panel support members and anchorage have been installed within alignment tolerances required by metal wall panel manufacturer.

          - Examine wall sheathing to verify that sheathing joints are supported by framing or blocking and that installation is within flatness tolerances required by metal wall panel manufacturer.

Retain subparagraph below with subparagraph above for systems that depend on air- or water-resistive barriers to prevent air infiltration or water penetration.

            - Verify that air- or water-resistive barriers have been installed over sheathing or backing substrate to prevent air infiltration or water penetration.

        - Examine roughing-in for components and systems penetrating metal panels to verify actual locations of penetrations relative to seam locations of metal panels before installation.

        - Proceed with installation only after unsatisfactory conditions have been corrected.

      - PREPARATION

        - Miscellaneous Supports: Install subframing, furring, and other miscellaneous panel support members and anchorages according to ASTM C 754 and metal panel manufacturer's written recommendations.

      - METAL PANEL INSTALLATION

        - General: Install metal panels according to manufacturer's written instructions in orientation, sizes, and locations indicated. Install panels perpendicular to supports unless otherwise indicated. Anchor metal panels and other components of the Work securely in place, with provisions for thermal and structural movement.

          - Shim or otherwise plumb substrates receiving metal panels.

          - Flash and seal metal panels at perimeter of all openings. Fasten with self-tapping screws. Do not begin installation until air- or water-resistive barriers and flashings that will be concealed by metal panels are installed.

          - Install screw fasteners in predrilled holes.

          - Locate and space fastenings in uniform vertical and horizontal alignment.

          - Install flashing and trim as metal panel work proceeds.

          - Locate panel splices over, but not attached to, structural supports. Stagger panel splices and end laps to avoid a four-panel lap splice condition.

          - Align bottoms of metal panels and fasten with blind rivets, bolts, or self-tapping screws. Fasten flashings and trim around openings and similar elements with self-tapping screws.

          - Provide weathertight escutcheons for pipe- and conduit-penetrating panels.

        - Fasteners:

          - Steel Panels: Use stainless-steel fasteners for surfaces exposed to the exterior; use galvanized-steel fasteners for surfaces exposed to the interior.

          - Aluminum Panels: Use stainless-steel fasteners for surfaces exposed to the exterior; use stainless-steel fasteners for surfaces exposed to the interior.

        - Metal Protection: Where dissimilar metals contact each other or corrosive substrates, protect against galvanic action as recommended in writing by metal panel manufacturer.

        - Lap-Seam Metal Panels: Fasten metal panels to supports with fasteners at each lapped joint at location and spacing recommended by manufacturer.

          - Lap ribbed or fluted sheets one full rib. Apply panels and associated items true to line for neat and weathertight enclosure.

          - Provide metal-backed washers under heads of exposed fasteners bearing on weather side of metal panels.

          - Locate and space exposed fasteners in uniform vertical and horizontal alignment. Use proper tools to obtain controlled uniform compression for positive seal without rupture of washer.

          - Install screw fasteners with power tools having controlled torque adjusted to compress washer tightly without damage to washer, screw threads, or panels. Install screws in predrilled holes.

          - Flash and seal panels with weather closures at perimeter of all openings.

Retain "Watertight Installation" Paragraph below for hydrostatic (watertight) panel installation; delete for water-shedding panel installations.

        - Watertight Installation:

          - Apply a continuous ribbon of sealant or tape to seal lapped joints of metal panels, using sealant or tape as recommend by manufacturer on side laps of nesting-type panels; and elsewhere as needed to make panels watertight.

          - Provide sealant or tape between panels and protruding equipment, vents, and accessories.

          - At panel splices, nest panels with minimum 6-inch (152-mm) end lap, sealed with sealant and fastened together by interlocking clamping plates.

        - Metal Liner Panels: Install panels on [exterior side of girts, with girts exposed to the interior] [interior side of girts with flush appearance on the inside].

        - Accessory Installation: Install accessories with positive anchorage to building and weathertight mounting, and provide for thermal expansion. Coordinate installation with flashings and other components.

          - Install components required for a complete metal panel system including trim, copings, corners, seam covers, flashings, sealants, gaskets, fillers, closure strips, and similar items. Provide types indicated by metal wall panel manufacturer; or, if not indicated, provide types recommended by metal panel manufacturer.

        - Flashing and Trim: Comply with performance requirements, manufacturer's written installation instructions, and SMACNA's "Architectural Sheet Metal Manual." Provide concealed fasteners where possible, and set units true to line and level as indicated. Install work with laps, joints, and seams that are permanently watertight.

          - Install exposed flashing and trim that is without buckling and tool marks, and that is true to line and levels indicated, with exposed edges folded back to form hems. Install sheet metal flashing and trim to fit substrates and achieve waterproof performance.

          - Expansion Provisions: Provide for thermal expansion of exposed flashing and trim. Space movement joints at a maximum of 10 feet (3 m) with no joints allowed within 24 inches (610 mm) of corner or intersection. Where lapped expansion provisions cannot be used or would not be sufficiently waterproof, form expansion joints of intermeshing hooked flanges, not less than 1 inch (25 mm) deep, filled with mastic sealant (concealed within joints).

      - FIELD QUALITY CONTROL

Retain "Testing Agency" Paragraph below to identify who shall perform tests and inspections. If retaining second option below, retain "Field quality-control reports" Paragraph in "Informational Submittals" Article.

        - Testing Agency: [Owner will engage] [Engage] a qualified testing agency to perform tests and inspections.

Retain "Water-Spray Test" Paragraph below to check system's resistance to water penetration. Revise indicated test-area requirements to suit Project.

        - Water-Spray Test: After installation, test area of assembly [shown on Drawings] [as directed by Architect] <Insert area> for water penetration according to AAMA 501.2.

Retain "Manufacturer's Field Service" Paragraph below to require a factory-authorized service representative to perform tests and inspections.

        - Manufacturer's Field Service: Engage a factory-authorized service representative to test and inspect completed metal wall panel installation, including accessories.

        - Remove and replace metal wall panels where tests and inspections indicate that they do not comply with specified requirements.

        - Additional tests and inspections, at Contractor's expense, are performed to determine compliance of replaced or additional work with specified requirements.

        - Prepare test and inspection reports.

      - CLEANING AND PROTECTION

        - Remove temporary protective coverings and strippable films, if any, as metal panels are installed, unless otherwise indicated in manufacturer's written installation instructions. On completion of metal panel installation, clean finished surfaces as recommended by metal panel manufacturer. Maintain in a clean condition during construction.

        - After metal panel installation, clear weep holes and drainage channels of obstructions, dirt, and sealant.

        - Replace metal panels that have been damaged or have deteriorated beyond successful repair by finish touchup or similar minor repair procedures.

END OF SECTION 074213.13